Spec.No：NWF-04F101

Issue Date：2008-3

Page：1 of 6

SPECIFICATION

FOR

SINGLEMODE OPTICAL FIBER

（FutureGuide-LWP）

Prepared ：  Xiaoquan Wang                  Approved：Vice-President Araki-

Spec.No：NWF-04F101

Issue Date：2008-3

Page：2 of 6

SPECIFICATION

FOR                                      SINGLEMODE OPTICAL FIBER

（Walsin Fujikura Designation: FutureGuide-LWP）

1.General

This specification covers a singlemode optical fiber optimized in the wavelength of 1310nm and 1550nrn region,but also can be used in the wavelength of 1383nm region,complying with the subcategory G652.C/D in the ITU-T recommendation G.652.March 2003

2.Specifications

Unless otherwise stated, the following characteristics are measured at ambient temperature.

(25±5℃)

2-1．Fiber Material

Core：Silica（SiO2） doped  with Germanium Dioxide（GeO2）

Cladding：Silica（SiO2）

Coating ：Dual layers of UV-cured acrylate（Non-colored）

2-2．Fiber Structure

Refer to Fig．l．

2-2-1.Dimensions

Mode field diameter：9.2±0.4μm at l310 nm

Cladding diameter： 125±0.7μm

Outer coating diameter：245±5μm

2-2-2 The fiber shall have a matched clad,step index profile,and the difference between the maximum refractive index of the core and that of the cladding is typically  0.36％（refer to Fig.2）

2-2-3.Mode field Concentricity Error

Not more than 0.6μm

2-2-4.Non Circularity of  The Cladding

Not more than l.0％

2-2-5.Cladding/Coating Concentricity Error

Not more than 12μm

2-2-6. Coloring

250±10μm

Spec.No：NWF-04F101

Issue Date：2004-3

Page：3 of 6

2-3.Optical Characteristics

The optical characteristics shall be measured on the coiled optical fiber length．

2-3-1.Attenuation（Refer to Fig. 3）

1310nm:     ≤ 0.35 dB／km

1550nm:     ≤ 0.22 dB／km

1383nm      ≤ 0.35 dB／km

1625nm:     ≤ 0.24 dB／km

2-3-2. Attenuation vs. Wavelength

The attenuation in a given wavelength range does not exceed the attenuation of the

reference wavelength（λ） by more than the valueα.

| Attenuation vs. Wavelength |
| --- |
| Range(nm) | Ref. λ(nm) | Max.Increased α（dB／km） |
| 1285 to 1330 1525 to 1575 | 1310 1550 | 0.05 |

2-3-3. Attenuation with Bending

The induced attenuation due to fiber  wrapped around a mandrel of a specified diameter  shown in the table below.

| Attenuation with Bending |
| --- |
| Mandrel Diameter(mm) | Number of Turn | Wavelength(nm) | Induced Attenuation(dB) |
| 32 50 60 60 | 1 100 100 100 | 1550 1310 1550 1625 | ≤0.5 ≤0.05 ≤0.05 ≤0.05 |

2-3-4.Attenuation Uniformity

No point discontinuity greater than 0.05 dB at either 1310nm or 1550nm in the OTDR trace．

2-3-5.Fiber Cut-off Wavelength λc

From 1150 to 1330 nrn, When measured on a 2 m fiber.

Spec.No：NWF-04F101

Issue Date：2004-3

Page：4 of 6

2-3-6. Chromatic Dispersion

≤3.5 ps／(km. n m)，When measured in the wavelength range of 1288 to l339。

≤5.3ps／(km. n m)， When measured in the wavelength range of 1271 to l360

≤18ps／(km. n m)， When measured at the wavelength of 1550nm

2-3-7. Zero-dispersion wavelengthλ0

1300≤λ0≤1324nm

2-3-8.Zero－dispersion slope

≤0.092 ps／km·nm2）

2-3-9.Polarization Mode Dispersion*

G.652.D≤0.2 ps/km1/2

2-3-10.Effective Group Index of Refraction Neff

1.4675 at l310 nm

1.4681 at l550 nrn

2-4 .Mechanical Characteristics

2-4-1．Proof  Test

The entire optical fiber length shall be tested with regard to the tensile strength in accordance with IEC 793-l. The screening test value is equal to or not less                    than135 kpsi（101.5kpsi= l％ elongation）．

2-5.Environmental Specifications：

Temperature Dependence of Attenuation

The induced attenuation from -60 to＋85℃ shall be ≤0.05 dB／km at either 1310 nrn or 1550 nm．

3.Packing and Storage Enviroment

3-1 The standard reel length is 25.2 km \24.8 km\24.6km\24.4km or in accordance with customers’ requirment at Walsin Fujikura’s discretion.The excess part is at least 50m.

The reel size shall be standardized by walsin Fujikura Ltd.

A Walsin Fujikura label(s) with the manufacture’s name,the production No., the type of fiber and the fiber length shall be shown on each reel．

3-2. Storage Enviroment (on the shipping spool)：

-40 to＋55℃, at＜ 98％ RH．

4.Measurement Data

If so requested by the customer, fiber data shall be transmitted electrically and precede each shipment ．

Spec.No：NWF-04F101

Issue Date：2004-3

Page：5 of 6

Fig.1 Structure of  UV-Cured Acrylate Fiber

Spec.No：NWF-04F201

Issue Date：2004-3

Page：6 of 6

Fig.3 Spectral Attenuation （Typical Fiber）